Selected parts of Goldstein book revised 1-2020;

Chapter 1  intro  read all

Chapter 2 sem modes   read entire chapter with the following in mind;

our jsm5310 1990s model SEM has a thermionic tungsten hairpin electron gun, our 2019 model jsm7200 has a Schottky field emission gun - concentrate on differences between these two sources - these dates do not necessarily correlate with gun type – you will still readily find thermionic tungsten source in a modern SEM    
(other sources are  the LaB6, or cold field emission sources)

eq 2.1, 2.2, 2.3, 2.4, 2.5, 2.6,  2.8 know relationships in these equations

eq 2.7  we will do this calculation in a different way in  lecture/lab

fig. 2-17, our system is as seen in (a) with virtual aperture

fig. 2-26 concentrate on tungsten thermionic

not necessary to study

eq. 2.6, 2.9, 2.10, 2.11

fig.  2.13, 2.14

all other figures are instructive, please try to understand them

Chapter 3  beam-specimen interactions  
p61-70 read all, do not memorize equations  (understand relationships)        note: fig 3.1,3.3,  3.4, 3.5   table 3.1

P71-80 eq. 3.7, figs. 3.8, 3.9
p80-81 read all, note:  fig 3.11

p88-97 read all,   note:   eq. 3.13	fig 3.17 (change y axes in a & b  to   # emitted e- )
		also note fig. 3.18, 3.19, 3.20, 3.22

Chapter 4 image formation

p99-110

note :  figs. 4.1, 4.2, 4.3, 4.4, 4.5

eq. 4.1 table 4.1

p111-131

note: 	figs.  4.9 , 4.13, 4.17, 4.19, 4.20

eq. 4.4, 4.5  table 4.2, 4.3

p132 section 4.3.2.2 less important

p134-139   only need to read about solid state BSE detector

p139-157

note: 	figs.   4.29, 4.30, 4.31, 4.35, 
table  4.5

eq.  4.8, 4.9, 4.10b

p 158-162

note:	figs. 4.36, 4.37 a-e (see a diagram of our BSE detector on website called JEOL5310lv_bse_detector)

p. 162-173  less important

p. 174-192

note: 	fig. 4.44  &  text p. 177  (contrast here is that from sample, not on screen.  They are related but not  identical.)

fig. 4.50  & text p. 182-184

Chapter 6  x-ray generation 

note:   figs. 6.1, 6.2, 6.5, 6.7, 6.9, 6.13, 6.14
	eq. 6.3

Chapter 7  x-ray measurements 

note:  figs. 7.3, 7.4 (we have Be window at MU), 7.6 (relate to dead time), 7.23, 7.28

ESPECIALLY GEOLOGY STUDENTS  

Chapter 9, pages 391-396 and 402-426