Residual Deposits

Bauxites

Definition:

Why Bauxites and laterites?

Conditions necessary for an economic bauxite deposit:

Low Fe, Ti, alkalis, and alkali earths

Characteristics:

- Irregular blankets several meters to tens of meters thick on top of their parent rock (usually but not always).

- Mineralogy and paragenetic sequence: Gibbsite (Al(OH)3)( boehemite (AlO(OH))+ diaspore (AlO(OH)).

- Can be redeposited

- Mined by open pit method.

- Age: mostly post-Mesozoic

- Main producers: Australia, Guinea, Jamaica, Brazil, India, Surinam and Balkan Republics.

Types of deposits:

1-High level or upland bauxites

- Directly on volcanic or plutonic rocks, no clay body in between.

- < 30 m in thickness

- In tropical and subtropical climates

- Porous and friable, often with relict textures

- Predominated by Gibbsite

- Weathering controlled by structures in parent rocks

- Examples: Ghana and Guinea

2- Low level peneplain bauxites

- Somewhat transported, separated from their parent rock by kaolinitic underclay

- ~ 9 m thick

- Along tropical coastlines

- Pisolitic textures

- Associated with detrital bauxites produced by fluvial and marine activity.

- South America, Australia, and Malaysia.

3- Karst Bauxites

- Oldest known

- In Eastern Europe

- On top of karst surfaces in limestone and dolomite

- Structureless, earthy, concretions, …. variable textures!

- Predominated by Boehemite

Origin:

Conditions necessary for formation of bauxites:

- favorable parent rock

- porosity

- high rainfall with intermittent dry spells

- good drainage

- tropical warm climate

- low relief

- long period of exposure

- vegetation

Mode of formation:

- Weathering

- In situ leaching of elements and enrichment of residue in Al

- Possible erosion and redeposition?

- Addition of eolian dust.

B- Laterites

- 6 – 20 m thick on top of mafic and ultramafic rocks.

- Nodular, red to yellow or brown hematite and goethite with as much as 20% Al2O3.

- Examples: Guinea, Guyana, Indonesia, Cuba and the Philippines.

C- Other Residual Deposits

1- Aurifeous laterites and bauxites

- In greenstone belts.

- Examples: Western Australia.

2- Ni and Co:

- 1-3 % Ni + Co in laterites on top of peridotites.

- Ore mineral: Garnierite (Ni,Mg)3Si2O5(OH)4.

- Example: New Caledonia.

3- Chromium:

- 3 % Cr in laterites on top of peridotites.

- Ore mineral: In hematite and goethite! (used in steel).

- Example: Western Australia.

4- Titanium:

- 12% Ti in soils (200 m thick) on top of alkalic igneous rocks.

- Ore mineral: Anatase.

- Example: Brazil (Parana Basin).

Supergene Enrichment

Definition

Conditions

- Active chemical weathering with ground level lowered by erosion

- Weathering under acidic (carbonated water) and oxidizing conditions

- Time

- Deep water table imposing reducing conditions

- Restricted to non-glacial terranes.

Zones:

Oxidizing zone ( Gossan

Reducing zone ( below water table.

Possible drop in grade with depth.

Structural Control

Examples:

Step 1:

Pyrite + H2O + CO2 + O2 ( Fe(OH)3 + H2SO4 + H2CO3

Ccp + H2O + CO2 + O2 ( Fe(OH)3 + CuSO4 + H2SO4 + H2CO3

Step 2:

PbS ( Cv (CuS) + anglesite

FeS2 ( Cc (Cu2S)

Ccp ( Cv