Volcanogenic Massive Sulfide Deposits (VMS)

Characteristics:

- Size and Grade: Usually small deposits with high grades of Cu, Zn, Pb, Au and Ag.

- Tonnages are widely variable.

- Metals: sources of Cu, Zn, Pb, ± Au ± Ag. High in Cd, As, Sb, Bi, Ba and Sn.

- Ore minerals: Chalcopyrite, sphalerite and galena + minor  arsenopyrite, magnetite, tetrahedrite, and tennantite. Vertical and lateral zonation is sometime cyclic.

- Gangue minerals: mainly Qz, ± Calcite. Barite and gypsum are common.

- Host rocks: Submarine volcanic rocks, ranging in composition from basalts to andesites and rhyolites.

- Shape and nature of Ore body: Conformable mounds or broadly stratiform lenses of massive sulfides usually overlying a zone of stockworks. Mounds usually overlain by layers of chert and barite. Commonly interlayered with carbonaceous shales.

- Zoning:

- Galena and pyrite in the upper half, with Ccp increasing into the stockwork.

- Ag in Galena increasing upwards

- Ba highest towards the top.

- (34S increases away from location of “vent” (see origin).

- Textures and primary structures:

- Colloform banding of sulfides with framboidal pyrite

- Metamorphism destroys these textures, and produces a granular ore.

- Soft – sediment structures

- Brecciation (crackle breccias).

- Graded bedding

- Wall rock alteration: Chloritization and sericitization.

- Age: variable, a few Archean deposits, most deposits Phanerozoic.

Types of VMS: (based on composition and predominant host rock)

- Cyprus: Cu, small, ophiolites (Fig. 1).

- Besshi: Cu – Zn, calcalkaline island arcs, thick greywacke sequences

- Kuroko: Cu – Zn – Pb: more felsic volcanics, large amounts of barite and gypsum (Fig. 2).

- Primitive: Cu – Zn, Precambrian terranes.

Origin:

Constraints:

- Fluids most likely circulating represent sea water (salinity, and O & H isotopes), possibly mixing with magmatic water (0 – 20%) (Fig. 3).

- Sulfides have mantle (34S values.

- Sulfates indicate a biogenic origin.

- Relatively low T (~ 100 – 300°C).

- Pb isotopic data is very uniform, similar to that of mantle.

- Ore deposits seem to be preferably associated with felsic volcanic rocks, rather than mafic ones.

- Analogy with Black smokers and white chimneys.

- Extreme telescoping.

Models:

- 1-Hydrothermal origin: Sea water circulating through thick pile of volcanics (Fig. 4). Four stages (cf. Evans p. 74; Fig. 5). Works best for Cyprus type deposits.

- Sea water mixing with magmatic (exhalative) water

- Stanton’s model: early magmatic origin, later affected by sea water circulation. Proposed to account for the higher concentration of the ores in intermediate and felsic volcanics rather than mafic ones.

- Long lived magmatically driven convection cells of sea water + addition of metal rich magmatic solutions from the heat source over short intervals of time.

- Exhalative origin: plumes of fluids deposit sulfides over a large area, unconsolidated sulfides then reworked into their mounds by submarine sliding, … etc.       (Figs. 6 - 8).