## Crystallography

A crystal is a solid object with a geometric shape that reflects a “long-range” regular internal structure (commonly with some element of symmetry).

# I- Space lattices

- Definition: The regular internal structure of a mineral is manifested by the existence of a space lattice, which is "an array of points in space that can be repeated indefinitely". All "points" in a lattice have identical environments (Fig. 1). In the case of a mineral or crystal, these "points" (also known as motifs) may be considered atoms, ions, or groups of atoms/ ions. Note that a lattice has no origin.

- A unit cell (Fig. 1) is the smallest number of "points" which completely define the space lattice. The repetition of those points or unit cells in a space lattice is performed by certain operations which build the space lattice.

Criteria used for the selection of unit cells:

- The smallest sized unit that retains the characteristics of the space lattice (Fig. 1b).

- Edges of the cell should coincide with symmetry axes (see below).

- Edges of the cell related to each other by the symmetry of the lattice.

- Building a space lattice: from motifs to lattices:

Motif ( Line lattice ( Plane lattice ( Space Lattice

- Operations: (a) elements of symmetry; (b) translations; (c) glide planes; (d) screw axes

A- Elements of symmetry:

Types:

i- Axes of rotation (1, 2, 3, 4 or 6): If during the rotation of a crystal around an axis one of the faces repeats itself two or more times, the crystal is said to have an axis of symmetry. Symmetry axes may be two fold (digonal) if a face is repeated twice every 360°, three fold (trigonal) if it is repeated three times, four fold (tetragonal) if it is repeated four times, or six fold (hexagonal) if that face is repeated 6 times. Figure 2a shows these relations.

ii- Center (n or i): If two similar faces lie at equal distances from a central point, the crystal is said to have a centre of symmetry (Fig. 2e).

iii- Planes (m): When one or more faces are the mirror images of each other, the crystal is said to have a plane of symmetry (Fig. 2f). Motifs related to each other by mirror planes are known as “enantiomorphs” (Fig. 4).

iv- Axes of rotary inversion (, ,  , or ): When two similar faces are repeated 2, 3, 4 or 6 times when the crystal is rotated 360° around an axis, but in such a way that these faces appear inverted. Therefore, if the face is repeated 2 times during a full rotation, the axis is known as a 2-fold rotary inversion axis, 3 times  3-fold rotary inversion, ..... etc. Figure 3 shows the types of rotary inversion axes. Note that axes of rotary inversion can also produce “enantiomorphs” (Fig. 4).

Equivalence of some symmetry elements:

( n (i)

( m

( 3 +

( 2 (note that this is not a perfect equivalency!)

( 3(m

N.B. Only rotary inversion axes of odd order imply the presence of symmetry centers.

Rules for combinations of rotations and mirrors: (Table 1)

- Rotary axes at 90° or 54°44’

- All operators must intersect at a point

- Rotary axes & mirrors are either perpendicular or parallel

- Intersection of 2 vertical mirror planes produces a digonal rotary axis

- Intersection of 3 vertical mirror planes produces a trigonal rotary axis

- Intersection of 4 vertical mirror planes at 45° produces a tetragonal rotary axis

- Intersection of 6 vertical mirror planes at 30° produces a hexagonal rotary axis

It was found that there are only 32 possible combinations of the above listed symmetry elements. These are known as “point groups” since the symmetry elements simply reproduce or repeat groups of points.

B- Translations (; Fig. 5): Think of a translation as an operation by which new motifs are generated in a new location; i.e. a means of “reproduction” for these motifs. Translations that reproduce a motif in that direction towards the reader in the plane of the paper are labeled by the vector “”, those moving to the right of the original motif “”, and those in a direction perpendicular to the plane of the paper “”. The lengths of these translation vectors are designated “ao”, “bo”, and “co”, respectively. The magnitude of these translations is normally on the order of 1 - 10 Å.

C- Glide plane (g): Is a compound symmetry operation that results from the combination of a mirror plane and a translation (Fig. 6; see Table 2 for compound symmetry).

D- Screw axes (xy): A screw axis forms by the combination of rotation and a translation. Depending on the type of rotation, there will be several types of screw axes (e.g. 2, 3, 4 & 6). Any of these screw axes will also be either right-handed or left-handed, and are given symbols as xy (e.g. 31) where if the ratio y/x is < 0.5 the axis is right handed, and if y/x > 0.5 the axis is left-handed (Fig. 7). It is essential that the rotational and screw axes have the same rotational angle (a phenomenon described as “isogonal”).

You will notice that there are no 5 - fold rotary, rotary inversion, or screw axes in crystals. This is simply because points or motifs related by five-fold symmetry will produce “objects” that are incapable of fitting together to produce closed space (Fig. 8).

The combination of the elements of symmetry with translations, glides and screw axes is what ultimately produces all possible crystal lattices, known as the 230 space groups. Breaking down this process into steps:

motifs translations in a plane> 5 (or 6) plane lattices symmetry in a plane>10 plane groups glide lines + mirror planes> 17 two-dimensional point groups glide planes + mirror planes + screw axes + elements of symmetry> 230 space groups.

# Crystal Morphology

  - Crystal Faces:

The regular internal structure of a mineral is manifested by the development of surfaces that define the shape of the crystal, and which may be related to one another by certain elements of symmetry. These surfaces are known as crystal faces.

- Bravais Law: Crystal faces are most likely to develop (fully, abundantly) along those planes with the highest density of lattice points. Bravais Law therefore states that the frequency by which a face is observed in a crystal is directly proportional to the number of “points” or “nodes” it intersects in a lattice (Fig. 9).

- Factors affecting the morphology of a crystal (conditions of growth):

- T

- P

- solutions available

- direction of solution flow

- availability of open space.

- Steno’s Law: The angles between these faces (known as the interfacial angles) are always constant for the same mineral (at the same temperature). Interfacial angles are measured using a goniometer (actually, the goniometer measures that angle that is complimentary to the interfacial angle; Fig. 10).

  - Crystallographic Axes & Interaxial angles:

In addition to "crystal faces" and "elements of symmetry", crystals can be described and classified on the basis of their "crystallographic axes" and "interaxial angles". Crystallographic axes are imaginary lines of reference inside a crystal that intersect at a common point (the crystal centre), and to which crystal faces can be referenced. Any crystal has either 3 or 4 crystallographic axes. The angles between these axes are known as the interaxial angles. Figure 11 shows the three standard crystallographic axes (a, b and c) and the nomenclature of the interaxial angles (,  and ). Note that a, b and c are the names given to the positive sides of the crystallographic axes, , , and  to the negative sides. Similarly, ,  and  apply only to those interaxial angles between the a, b and c (not , , and ).

    - Criteria used for the selection of the crystallographic axes:

- In crystals that lack sufficient symmetry, axes are selected to coincide with the lines of intersection between the major (largest) crystal faces (Fig. 12).

- Ideally, they should be parallel to the edges of the unit cell, and their lengths should be proportional to the edges of the unit cell.

- Either 3 or 4 in number.

- Perpendicular wherever possible

- As much as possible, they should coincide with the symmetry axes, and be perpendicular to the symmetry planes.

- For monoclinic systems (see below), +a is selected so that ( > 90°. For triclinic systems, ( and ( are each > 90°.

- In practice, crystallographic axes are determined from X-ray measurements!!

C- Relationship between crystal faces and crystallographic axes: Indexing the crystal faces

- Intercepts: Points of intersection of the face with the crystallographic axes.

- Coordinates: Actual distances of the intercepts of a face with the crystallographic axes expressed in some unit of measurement (e.g. mm, cm, inches, … etc.; Fig13)

- Parameters: Distances; i.e. coordinates of one face divided by those of another to which it is parallel. Expressed as: 2a:4b:1c. They are intercepts referenced to axes a, b and c.

- The unit face: Is a face that intersects all three crystallographic axes, and is arbitrarily assigned the parameters 1a: 1b: 1c. In the event that several faces intersect all three axes in the crystal, the face with the largest area is selected as the unit face.

- Indices (Miller Indices): Are whole numbers that represent the reciprocals of parameters after clearing the fractions (by multiplying by one or more factors).

- Law of rational indices (Law of Haüy): The position of one face on a crystal can always be referred to that of another face on the same crystal by ratios, which may be expressed in small whole numbers that seldom exceed 3.

- Zones: All faces whose lines of intersection are parallel are considered a zone. The zone axis is a line through the center of a crystal to which the edges of intersection of faces in a zone are parallel (Fig. 14).

    - Crystal Forms:

Two or more faces having the same geometric relations to the crystallographic axes, and the same shape, and which are related to each other by some element of symmetry in a crystal constitute a crystal form, (defined as an assemblage of one or more faces which may partially or completely constitute a crystal exterior). A crystal may thus consist of one or more forms (Fig. 15).

### III- Towards a classification of crystals: Systematic Crystallography

As mentioned above, there are only 32 possible combinations of the symmetry elements (excluding the screw axes and glide planes) that can be referred to sets of axes intersecting at a common point (i.e. crystallographic axes). Accordingly, the external geometry of any crystal must correspond to one of these 32 sets, known as "classes". Many of these classes share some fundamental element or elements of symmetry. Therefore, these classes that have common symmetry elements are grouped together into a "crystal system", so that all 32 crystal classes fall into seven crystal systems.

    - The Crystal Systems

The crystal classes are grouped into seven crystal systems based on the following criteria:

a) relative lengths of the crystallographic axes

b) number of crystallographic axes

c) values of the interaxial angles

d) some essential element of symmetry

The seven crystal systems are (Fig. 16; Table 3):

(1) The Cubic system: Three crystallographic axes, a = b = c,  =  =  = 90. Essential element of symmetry is a three-fold rotary or rotary inversion axis.

(2) The Tetragonal system: Three crystallographic axes, a = b  c,  =  =  = 90. Essential element of symmetry is a four-fold rotary or rotary inversion axis.

(3) The Trigonal system: Four crystallographic axes, three of which are equal and coplanar and at angles of 120°, fourth axis "c" is perpendicular to the other three axes, and is characterized by commonly being a three fold axis of symmetry.

(4) The Hexagonal system: Four crystallographic axes, three of which are equal and coplanar (a1, a2, a3) and at angles of 120°, fourth axis (c) is perpendicular to the other three axes, and is characterized by being a six fold axis of symmetry.

(5) The Orthorhombic system: a  b  c,  =  =  = 90. Essential element of symmetry is a two-fold rotary axis. Some debate over choice of axes! Generally, c < a < b!!!

(6) The Monoclinic system: a  b  c,  =  = 90,  > 90. Essential element of symmetry is a two fold rotary axis or a plane. The 2-fold rotational axis or the direction perpendicular to the mirror plane is usually taken as the b axis, the a axis is inclined to the front (( > 90°), and c is vertical.

(7) The Triclinic system: a  b  c,     . No essential element of symmetry. Additional criteria: As much as possible, ( and ( should be both > 90°. The most pronounced zone should be vertical. The axis of this zone is then taken as “c”. {001} should slope forward and to the right. In general, c<a<b!

    - The Hermann Mauguin Symbols

Each of the elements of symmetry is designated by a unique alphanumeric symbol. If the same symmetry element occurs more than once in a crystal, then it is designated by the symbol raised to the power of number of occurrences. A string of Hermann Mauguin symbols for a crystal therefore completely summarizes its symmetry. Note that a shorthand form of these symbols largely ignores the number of times an element is repeated (as this can be guessed with little trouble, and some experience). We will stick to the long-form in our class.

    - Crystal classes & crystal systems

To clarify the relationship between the crystal systems and classes, let us consider the cubic system. This system, defined by having three equal crystallographic axes, and interaxial angles of 90°, is also characterized by having a three-fold rotary axis of symmetry. The cubic system has five distinct classes, each characterized by a unique set of symmetry elements. Among this set of symmetry elements is the three-fold rotary axis; the essential element of symmetry for the cubic system. The tetragonal system has seven classes, all with a four - fold or four - fold rotary inversion axis of symmetry, .... etc. Table 4 lists the fundamental features of each one of the seven crystal systems as well as the classes belonging to each system.

Crystal forms: Each crystal system is characterized by a number of specific forms. Some of these forms are unique to a particular system, whereas others can occur in several different systems. Within a system, forms characteristic of a higher symmetry class can exist in crystals belonging to a lower symmetry class, but not the reverse! An example is the Octahedron, characteristic of the hexoctahedral (holohedral) class (4/m2/m), can actually exist in the Diploidal (2/m) class, but the pyritohedron (characteristic of the Diploidal class) cannot exist in the holohedral class. Forms that are common to most crystal systems are: Pedion, Pinacoid, Dome, Sphenoid, Prism, and Pyramid. Figure 15a shows some common forms in the seven systems, whereas Fig. 15b shows two examples of complicated combinations of some forms in the cubic system. These two figures show that in any system, a crystal may be made of one or more forms. For a full list and illustration of all 48 possible forms, please refer to your textbook.

- The Bravais Lattices

Investigating the shapes and types of unit cells for all crystal structures belonging to the different crystal systems reveals that there are only 14 possible different unit cells which when repeated through symmetry operations will define all possible lattices. These different unit cells are known as Bravais Lattices, and are really four basic types of unit cells applied to the 7 crystal systems (to yield the 14 Bravais lattices; Fig. 17). The four basic types are:

Primitive (P), Body centered (B or I), Face centered (F), and End – Centered (E or C).

Knowing that Halite is cubic, can you figure out its type of Bravais Lattice? Refer to Fig. 1b to help you out.

- Relationship between the 230 Space groups and the 32 Crystal classes (Point groups):

- A point group implies that one point within the lattice remains fixed.

- Point groups are defined on the basis of all possible combinations of the elements of symmetry ( there are 32 possible combinations.

- Space groups are defined by the combination of elements of symmetry, glide planes and screw axes, along with a definition of the space (Bravais) lattice (P, A, B, C, I, F, …etc.)

- Space groups and point groups of the same system have to be isogonal.

- The point group can therefore be derived from the space group by eliminating the lattice type, screw axes, and glide planes.

- You can figure out the crystal system easily from its point group or space group. Simply eliminate the space lattice symbol, replace every screw axis by its isogonal regular axis of symmetry, and replace every glide plane by the symbol “m” for the mirror. Now you have the point group (crystal class)!

- The Stereographic projection

The stereographic projection is a 2-D graphical representation of the symmetry elements of a crystal (or a crystal class), as well as the relative locations of all its faces. As such, it is much easier to construct and read compared to a 3-D drawing of a crystal (the most common type of 3-D view is known as the clinographic view).

Steps and rules for constructing a stereographic projection:

  - Imagine that the crystal is located in a large sphere. From the center of each face of the crystal, draw a straight line perpendicular to this face until it reaches the surface of the enclosing sphere. Each one of these lines is known as a pole, and each face will now be represented by a point on the surface of the sphere. This is known as a spherical projection (Fig. 18).

  - Imagine cutting the sphere into two halves along the equator of this sphere. You now have 2 hemispheres: a northern hemisphere and a southern one.

  - The equatorial surface of this sphere (a large circle with the radius of the sphere) is now going to be used as the projection plane. This circle is known as the “primitive circle”. All other circles through the sphere that maintain its same radius are known as “great circles”. These may represent mirror planes.

  - Every point in the northern hemisphere representing a crystal face can now be projected onto the stereographic projection by drawing a line from each of these points to the south pole of the original sphere. The point of intersection of this line with the projection plane marks the actual location or projection of this face, and is marked with an “x” (Fig. 19).

  - Points in the southern hemisphere representing crystal faces can be projected onto the same plane by drawing lines from these points to the north pole of the original sphere. The points of intersection of these lines with the projection plane mark the location or projection of these faces, and are marked with an “o”.

  - The location of the crystallographic axes is marked by lines with arrow feathering at their ends (Fig. 20). The c axis will be located at the center of the projection, b to the right, and “a” at the bottom (in front; Fig. 20).

  - Axes of rotation or rotary inversion (represented by points) are designated with their usual symbols at these points (see above; Fig. 20).

  - Symmetry planes are indicated by solid lines (for planes coinciding with or containing the c-axis), a solid circle coinciding with the primitive circle (if the plane is perpendicular to the c axis) or solid arcs (representing great circles or planes oriented at an angle of 45° to the c-axis).

  - The size and shape of a crystal face projected are unimportant (and not represented) on a stereographic projection, but its position relative to other faces is maintained.

  - All faces of the same zone will be represented by points lying on the same great circle. A face common to 2 zones plots as a point at the intersection of two great circles.

  - Dashed arcs and circles on a stereographic projection represent great circles, which do not coincide with symmetry planes.

Figures 20 and 21 show stereographic projections and elements of symmetry for the hextetrahedral class, and some of the forms for the hexoctahedral class. For a detailed explanation of how interfacial angles are used to plot crystal faces on the stereographic projection with the aid of a Wulf net (Fig. 22), refer to pages 241 – 248 of Klein (2002).

- Twinning:

Twin Rules:

1- an axis of even fold symmetry can never become a twin axis. Only a 3 – fold symmetry axis can serve as a twin axis

2- Twinning planes never coincide with symmetry planes in either part of the compound crystal.

3- Twins that develop in classes with a center of symmetry have both a twin axis and a twinning plane perpendicular to it.

4- Twinning results in increased symmetry.

Common Twin Laws:

| System | Type | Name | Twin law | Example | Figure |
| --- | --- | --- | --- | --- | --- |
| Cubic | Contact | Spinel | plane: {1}; axis: [11] | Spinel | 23 |
| Cubic | Penetration | Iron cross | axis: [001] | Pyrite | 24 |
| Tetragonal | Contact | Geniculated (elbow) | plane: {011} | Cassiterite, Rutile & Zircon | 25 |
| Trigonal | Contact | Calcite | plane: {101} | Calcite | 26 |
| Trigonal | Cyclic | Polysynthetic | plane: {012} | Calcite | 27 |
| Trigonal | Contact | Brazil | plane: {110} | Quartz | 28 |
| Trigonal | Contact | Dauphiné | axis: [0001] | Quartz | 29 |
| Orthorhombic | Cyclic | Cyclic | plane: {110} | Aragonite | 30 |
| Orthorhombic | Penetration | Cross twins | plane: {031} | Staurolite | 31a |
| Orthorhombic | Penetration | Oblique cross | plane: {231} | Staurolite | 31b |
| Monoclinic | Contact | Simple | axis [001] | Orthoclase | 32a |
| Monoclinic | Penetration | Carlsbad | axis [001] | Orthoclase | 32b |
| Monoclinic | Contact | Manebach | plane: {001} | Orthoclase | 33 |
| Monoclinic | Contact | Baveno | plane: {021} | Orthoclase | 34 |
| Monoclinic | Contact | Swallow tail | plane: {100} | Gypsum | 35 |
| Triclinic | Cyclic | Albite or polysynthetic | plane: {010} | Plagioclase feldspars | 36 |
| Triclinic | Cyclic | Pericline | axis: [010] | Plag felds. | 37 |